Support Information

Wet Torrefaction of Biomass Waste into Value-Added Liquid Product (5-HMF) and High Quality Solid Fuel (Hydrochar) in a Nitrogen Atmosphere

Andrii Kostyniuka, Blaž Likozara,b,c,d

aDepartment of Catalysis and Chemical Reaction Engineering, National Institute of Chemistry, Hajdrihova 19, Ljubljana, 1001, Slovenia

bFaculty of Polymer Technology, Slovenj Gradec 2380, Slovenia

cPulp and Paper Institute, Bogišićeva 8, Ljubljana 1000, Slovenia

dFaculty of Chemistry and Chemical Technology, University of Ljubljana, Večna pot 113, Ljubljana 1000, Slovenia

Table S1. Elemental analysis of the WT WCPR samples after 15 min as compared to the WCPR.

| Samples | T, °C | t, min | H2O/WCPR ratio | Elemental analysis (wt%) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | C | H | N | S |
| WCPR | − | − | − | 48.3 | 6.2 | 0.1 | 0.5 |
| WT_WCPR_180 | 180 | 15 | 10 | 50.1 | 6.1 | 0.2 | 0.0 |
| WT_WCPR_200 | 200 | 15 | 10 | 50.2 | 6.0 | 0.2 | 0.0 |
| WT_WCPR_220 | 220 | 15 | 10 | 50.5 | 6.0 | 0.8 | 0.0 |
| WT_WCPR_240 | 240 | 15 | 10 | 64.2 | 4.9 | 0.2 | 0.0 |
| WT_WCPR_260 | 260 | 15 | 10 | 66.0 | 4.7 | 0.2 | 0.0 |

Table S2. Elemental analysis of the WT WCPR samples after 60 min as compared to the WCPR.

| Samples | T, °C | t, min | H2O/WCPR ratio | Elemental analysis (wt%) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | C | H | N | S |
| WCPR | − | − | − | 48.3 | 6.2 | 0.1 | 0.5 |
| WT_WCPR_180 | 180 | 60 | 10 | 49.7 | 5.9 | 0.2 | 0.0 |
| WT_WCPR_200 | 200 | 60 | 10 | 50.1 | 5.9 | 0.2 | 0.0 |
| WT_WCPR_220 | 220 | 60 | 10 | 55.4 | 5.5 | 0.2 | 0.0 |
| WT_WCPR_240 | 240 | 60 | 10 | 65.3 | 4.7 | 0.2 | 0.0 |
| WT_WCPR_260 | 260 | 60 | 10 | 67.6 | 4.6 | 0.2 | 0.0 |

Table S3. HHV, enhancement factor and atomic ratios of the WT WCPR samples after 15 min as compared to the WCPR.

| Samples | T, °C | t, min | H2O/WCPR ratio | HHV, kJ/kg | Enhancement factor | Atomic ratio | CE1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | H/C |  |
| WCPR | − | − | − | 19179 | 1.00 | 1.5 | 1.00 |
| WT_WCPR_180 | 180 | 15 | 10 | 19962 | 1.04 | 1.5 | 1.04 |
| WT_WCPR_200 | 200 | 15 | 10 | 19950 | 1.04 | 1.4 | 1.04 |
| WT_WCPR_220 | 220 | 15 | 10 | 20170 | 1.05 | 1.4 | 1.04 |
| WT_WCPR_240 | 240 | 15 | 10 | 25555 | 1.33 | 0.9 | 1.33 |
| WT_WCPR_260 | 260 | 15 | 10 | 26232 | 1.37 | 0.9 | 1.37 |

1CE – carbon enrichment.

Table S4. HHV, enhancement factor and atomic ratios of the WT WCPR samples after 60 min as compared to the WCPR.

| Samples | T, °C | t, min | H2O/WCPR ratio | HHV, kJ/kg | Enhancement factor | Atomic ratio | CE1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | H/C |  |
| WCPR | − | − | − | 19179 | 1.00 | 1.5 | 1.00 |
| WT_WCPR_180 | 180 | 60 | 10 | 19712 | 1.03 | 1.4 | 1.03 |
| WT_WCPR_200 | 200 | 60 | 10 | 19906 | 1.04 | 1.4 | 1.04 |
| WT_WCPR_220 | 220 | 60 | 10 | 21998 | 1.15 | 1.2 | 1.15 |
| WT_WCPR_240 | 240 | 60 | 10 | 25912 | 1.35 | 0.9 | 1.35 |
| WT_WCPR_260 | 260 | 60 | 10 | 26878 | 1.40 | 0.8 | 1.40 |

1CE – carbon enrichment.

Corresponding authors:

E-mail address: andrii.kostyniuk@ki.si (Andrii Kostyniuk)

E-mail address: blaz.likozar@ki.si (Blaž Likozar)