Catalytic Wet Torrefaction of Biomass Waste into Bio-Ethanol, Levulinic Acid, and High Quality Solid Fuel

Andrii Kostyniuka, Blaž Likozara,b,c,d

aDepartment of Catalysis and Chemical Reaction Engineering, National Institute of Chemistry, Hajdrihova 19, Ljubljana, 1001, Slovenia

bFaculty of Polymer Technology, Slovenj Gradec 2380, Slovenia

cPulp and Paper Institute, Bogišićeva 8, Ljubljana 1000, Slovenia

dFaculty of Chemistry and Chemical Technology, University of Ljubljana, Večna pot 113, Ljubljana 1000, Slovenia

Table S1

Composition of the wood cellulose pulp residue (WCPR).

| Glucan (wt% dry) | Lignin AIL − ash | Lignin ASL | Ash | Total |
| --- | --- | --- | --- | --- |
| 62.26 | 30.90 | 0.14 | 1.4 | 94.7 |
| Lignin AIL | Acid Insoluble Lignin |  |  |  |
| Lignin ASL | Acid Soluble Lignin |  |  |  |

(a)

(b)

(c)

Fig. S1. Photograph of the stainless steel (Parr, 5000 Multiple Reactor System) batch reactors utilized for WT of WCPR – (a); layout diagram of multiple reactor system – (b); 5050/5051 vessel body diagram, PTFE and O-ring seals – (c).

Table S2

Chemical analysis and structural properties of the H-ZSM-5 zeolite catalyst.

| Catalyst | SiO2/Al2O3 ratio | SBETa (m2/g) | Smicroa (m2/g) | Smesoa (m2/g) | Vmicrob (cm3/g) | Vtotalb (cm3/g) | Vmesob (cm3/g) | PDc (nm) | Average crystallite sized (nm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H-ZSM-5 | 30 | 348 | 230 | 118 | 0.12 | 0.25 | 0.13 | 6.4 | 50.3 |

aBET method. bt-plot method. cPD − average pore diameter measured from the desorption branch according to the BJH method. dThe crystallite size and relative crystallinity were calculated from the seven most intensive diffraction peaks of XRD spectra.

Table S3

Acid properties of the H-ZSM-5 zeolite catalyst.

| Acid site density by NH3-TPD (mmolNH3/gcat) |  |  |  | Diversity of acid sites by pyridine-DRIFTS (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Total | Weaka | Strongb | Strong/Weak | BAS | LAS | BAS/LAS ratio |
| 0.87 | 0.43 | 0.44 | 1.0 | 71.5 | 28.5 | 2.51 |

a − determined at average temperature T = 202.2 °C.

b − determined at average temperature T = 396.6 °C.

BAS − Brönsted acid sites.

LAS − Lewis acid sites.

Table S4. SEM-EDX analysis of the WCPR, WT_WCPR and the WT+ZSM-5 samples.

| WCPR |  |  |  |
| --- | --- | --- | --- |
| Element | Scan 1 (wt%) | Scan 2 (wt%) | Scan 3 (wt%) |
| C | 57.97 | 58.57 | 57.97 |
| O | 41.69 | 41.27 | 41.85 |
| Si | 0.06 | ‒ | 0.06 |
| Al | ‒ | ‒ | ‒ |
| S | 0.14 | ‒ | ‒ |
| Ca | 0.13 | ‒ | 0.13 |
| WT_WCPR |  |  |  |
| C | 59.42 | 59.40 | 58.75 |
| O | 40.58 | 40.60 | 41.25 |
| Si | ‒ | ‒ | ‒ |
| Al | ‒ | ‒ | ‒ |
| S | ‒ | ‒ | ‒ |
| Ca | ‒ | ‒ | ‒ |
| WT+ZSM-5 |  |  |  |
| C | 45.68 | 43.87 | 45.26 |
| O | 42.70 | 43.95 | 42.01 |
| Si | 10.65 | 11.18 | 11.68 |
| Al | 0.86 | 0.88 | 0.91 |
| S | ‒ | ‒ | ‒ |
| Ca | 0.12 | 0.11 | 0.13 |

Corresponding authors:

E-mail address: andrii.kostyniuk@ki.si (Andrii Kostyniuk)