Assessments of Sustainable Chemicals and Bioenergy Potentials of Selected Lignocellulosic Biomass Feedstocks in Poland via Physicochemical Characterisation and Pyrolysis

Omar Mohammad1, Muhammad Khan1, Hilal Unyay2, Radosław Ślężak2, Szymon Sufa2, Jude A. Onwudili1 *

1 Energy and Bioproducts Research Institute, College of Engineering and Physical Sciences, Aston University, Aston Triangle, Birmingham B4 7ET, UK

2 Faculty of Process and Environmental Engineering, Lodz University of Technology, Wolczanska 213 str., 90-924 Lodz, Poland; hilal.unyay@dokt.p.lodz.pl (H.U.) 0000-0002-4464-7741, radoslaw.slezak@p.lodz.pl (R.S.) 0000-0002-2025-8477, szymon.szufa@p.lodz.pl (S.S.) 0000-0002-7287-0553

Table S1. TGA-DTG peaks positions for different raw materials under nitrogen.

| Material | 1st DTG (°C) | DTG (wt.% °C–1) | Mass loss (wt.%) | 2nd DTG (°C) | DTG (wt.% °C–1) | Mass loss (wt.%) |
| --- | --- | --- | --- | --- | --- | --- |
| OXY | 202.3 | 1.2 | 9.2 | 322.7 | 11.2 | 46.8 |
| PIN | - | - | - | 370.2 | 15.3 | 63.5 |
| SOR | 230.8 | 2.4 | 13.0 | 341.7 | 8.3 | 49.5 |
| FOR | - | - | - | 351.2 | 7.2 | 42.2 |
| COF | 224.5 | 16 | 11.9 | 313.2 | 9.7 | 40.0 |

Table S2. Average weight percentage (wt. %) of gaseous products based on the overall mass balance.

| Material | Temp. (°C) | H₂ | CH₄ | C₂Hn | CO | CO₂ |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Weight percentage (wt.%) |  |  |  |  |
| OXY | 400 | 0.00 | 0.09 | 0.09 | 2.50 | 9.92 |
|  | 500 | 0.01 | 0.57 | 0.69 | 3.60 | 12.27 |
|  | 600 | 0.03 | 1.05 | 1.58 | 6.12 | 12.27 |
| PIN | 400 | 0.00 | 0.21 | 0.08 | 4.05 | 8.54 |
|  | 500 | 0.02 | 1.10 | 0.57 | 6.09 | 7.61 |
|  | 600 | 0.08 | 2.94 | 1.59 | 12.16 | 10.17 |
| SOR | 400 | 0.00 | 0.10 | 0.07 | 3.83 | 12.52 |
|  | 500 | 0.00 | 0.63 | 0.58 | 4.92 | 14.97 |
|  | 600 | 0.02 | 1.04 | 1.56 | 6.82 | 16.87 |
| COF | 400 | 0.00 | 0.00 | 0.04 | 0.50 | 9.56 |
|  | 500 | 0.01 | 0.22 | 0.79 | 2.38 | 12.17 |
|  | 600 | 0.03 | 1.11 | 3.80 | 5.63 | 11.44 |
| FOR | 400 | 0.01 | 0.10 | 0.06 | 1.80 | 8.53 |
|  | 500 | 0.01 | 0.49 | 0.39 | 2.80 | 9.85 |
|  | 600 | 0.04 | 0.85 | 1.09 | 5.63 | 8.39 |

Table S3. Liquid composition from the flash pyrolysis of different raw materials at various temperatures.

| Category of Compounds (% of peak area) | OXY |  |  | PIN |  |  | SOR |  |  | FOR |  |  | COF |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 400 | 500 | 600 | 400 | 500 | 600 | 400 | 500 | 600 | 400 | 500 | 600 | 400 | 500 | 600 |  |
| Nitrogen-containing | 3 | 3 | 2 | 4 | 5 | 2 | 3 | 0 | 2 | 2 | 3 | 1 | 9 | 7 | 9 |  |
| Carboxylic acids | 0 | 1 | 3 | 3 | 7 | 3 | 1 | 0 | 1 | 4 | 1 | 2 | 41 | 39 | 24 |  |
| Carbonyls | 6 | 20 | 14 | 15 | 13 | 8 | 10 | 13 | 9 | 10 | 6 | 12 | 8 | 7 | 9 |  |
| Alcohols | 2 | 4 | 5 | 6 | 3 | 0 | 3 | 1 | 2 | 3 | 4 | 3 | 4 | 5 | 3 |  |
| Phenols | 53 | 44 | 38 | 30 | 36 | 37 | 40 | 44 | 38 | 39 | 37 | 33 | 6 | 8 | 11 |  |
| Esters | 6 | 3 | 6 | 5 | 2 | 3 | 8 | 6 | 7 | 2 | 3 | 2 | 6 | 4 | 10 |  |
| Hydrocarbons | 7 | 5 | 9 | 0 | 0 | 1 | 2 | 2 | 3 | 2 | 3 | 13 | 5 | 5 | 9 |  |
| Sugars | 7 | 6 | 7 | 23 | 25 | 32 | 5 | 4 | 4 | 27 | 32 | 24 | 13 | 14 | 9 |  |
| Furans | 1 | 1 | 1 | 0 | 0 | 2 | 13 | 13 | 15 | 2 | 1 | 2 | 0 | 0 | 1 |  |
| Unknowns | 15 | 14 | 14 | 15 | 9 | 12 | 16 | 15 | 19 | 10 | 10 | 7 | 8 | 11 | 14 |  |