Wet Torrefaction of Biomass Waste into High Quality Hydrochar and Value-Added Liquid Products Using Different Zeolite Catalysts

Andrii Kostyniuka, Blaž Likozara,b,c,d

aDepartment of Catalysis and Chemical Reaction Engineering, National Institute of Chemistry, Hajdrihova 19, Ljubljana, 1001, Slovenia

bFaculty of Polymer Technology, Slovenj Gradec 2380, Slovenia

cPulp and Paper Institute, Bogišićeva 8, Ljubljana 1000, Slovenia

dFaculty of Chemistry and Chemical Technology, University of Ljubljana, Večna pot 113, Ljubljana 1000, Slovenia

S1. Materials

The zeolite catalysts obtained from commercial suppliers include H-ZSM-5 (SiO2/Al2O3 = 30, Zeolyst International), H-Beta (SiO2/Al2O3 = 28, Tosoh Corporation), H-Y (SiO2/Al2O3 = 5.1, Tosoh Corporation), H-USY (SiO2/Al2O3 = 10, Tosoh Corporation), and H-Mordenite (SiO2/Al2O3 = 15, Tosoh Corporation). All employed zeolites underwent a calcination process at 550 °C (10 °C/min) in the air for 6 hours to eliminate impurities. The specific chemicals and their respective suppliers are outlined below: ethanol (>99.8%, Merck), levulinic acid (99.5%, Merck), hydroxyacetone (99.5%, Merck), 5-hydroxymethylfurfural (>97 wt%, Carbosynth, FH10853), 5-methylfurfural (99 wt%, Merck), furfural (>99 wt%, Merck), methanol (>99.9%, Merck), guaiacol (99.5%, Merck), 2,3-butanedione (99%, Merck), phenol (≥98.5%, Merck), 2-butanone (99.5%, Merck), acetone (>99.5%, Merck), acetoin (>99.5%, Merck), acetic acid (>99.7%, Merck), cyclopentenone (>99%, Merck), acetylacetone (>99%, Merck), 2,5-hexanedione (>99.5%, Merck), hydrogen (5.0, Messer, Germany), nitrogen (5.0, Messer, Germany), helium (5.0, Messer, Germany).

Table S1

Composition of the wood cellulose pulp residue (WCPR).

| Glucan (wt% dry) | Lignin AIL − ash | Lignin ASL | Ash | Total |
| --- | --- | --- | --- | --- |
| 62.26 | 30.90 | 0.14 | 1.4 | 94.7 |
| Lignin AIL | Acid Insoluble Lignin |  |  |  |
| Lignin ASL | Acid Soluble Lignin |  |  |  |

Fig. S1. Stainless steel (Parr) batch reactors utilized for WT of WCPR.

Table S2

Chemical analysis and structural properties of the different zeolite catalysts.

| Catalyst | SiO2/Al2O3a ratio | SBETb (m2/g) | Smicrob (m2/g) | Smesob (m2/g) | Vmicroc (cm3/g) | Vtotalc (cm3/g) | Vmesoc (cm3/g) | PDd (nm) | Average crystallite sizee (nm) | Particle sizef (nm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H-ZSM-5 | 30.0 | 348 | 230 | 118 | 0.12 | 0.25 | 0.13 | 6.4 | 44.8 | 174 |
| H-USY | 10.0 | 667 | 559 | 108 | 0.29 | 0.46 | 0.17 | 8.3 | 54.6 | 365 |
| H-Y | 5.1 | 665 | 606 | 59 | 0.32 | 0.36 | 0.04 | 5.2 | 59.0 | 713 |
| H-Mordenite | 15.0 | 418 | 381 | 37 | 0.20 | 0.23 | 0.03 | 4.1 | 63.6 | 1011 |
| H-Beta | 28.0 | 549 | 441 | 108 | 0.23 | 0.32 | 0.09 | 5.2 | 16.7 | 379 |

aSi and Al content according to ICP-OES. bBET method. ct-plot method. dAverage pore diameter measured from the desorption branch according to the BJH method. eThe crystallite size was calculated from XRD data using at least the 5 most intense peaks; fParticle size according to HRSEM.

Table S3

Acid properties of the different zeolite catalysts.

| Catalyst | Acidity by NH3-TPD (mmolNH3/gcat) |  |  | Acidity by Pyr-DRIFTS (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Total | Weak | Strong | CBAS | CLAS | BAS/LAS ratio |
| H-Beta | 1.78 | 0.81 | 0.97 | 54.9 | 45.1 | 1.2 |
| H-ZSM-5 | 1.75 | 0.95 | 0.80 | 71.5 | 28.5 | 2.5 |
| H-Y | 1.93 | 0.97 | 0.96 | 50.6 | 49.4 | 1.0 |
| H-USY | 2.08 | 0.83 | 1.25 | 55.0 | 45.0 | 1.2 |
| H-Mordenite | 4.69 | 2.23 | 2.46 | 60.1 | 39.9 | 1.5 |

BAS − Brönsted acid sites.

LAS − Lewis acid sites.

Table S4

Proximate and elemental analysis, BET surface area, pore diameter (PD), crystalline index, and crystallite size of the WT+ZSM-5 samples as compared to the WCPR.

| Samples | T, °C | t, min | H2O/WCPR ratio | Proximate analysis (wt%) |  |  |  | Elemental analysis (wt%) |  |  |  |  |  | BET surface area, m2/g | PD3, nm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Moisture | VM1 | FC2 | Ash+Si+Al | C | H | O | N | S | Si+Al |  |  |
| WCPR | – | – | – | 1.5 | 75.5 | 19.8 | 3.2 | 48.3 | 6.2 | 40.3 | 0.1 | 0.5 | 0 | 3.4 | 39.4 |
| WT_WCPR_220 | 220 | 60 | 10 | 1.2 | 76.5 | 21.3 | 1.0 | 55.4 | 5.5 | 34.5 | 0.2 | ‒ | 0 | 3.5 | 37.9 |
| WT+ZSM-5 | 220 | 60 | 10 | 2.0 | 32.1 | 29.5 | 36.4 | 72.6 | 3.1 | 19.0 | 0.1 | 0.1 | 5.1 | 24.6 | 23.5 |
| WT+Beta | 220 | 60 | 10 | 4.8 | 29.5 | 30.6 | 35.1 | 71.9 | 3.1 | 16.9 | 0.1 | ‒ | 8.0 | 22.7 | 18.5 |
| WT+Y | 220 | 60 | 10 | 7.9 | 35.6 | 27.9 | 28.6 | 65.5 | 4.0 | 19.2 | 0.1 | ‒ | 11.2 | 80.6 | 14.7 |
| WT+USY | 220 | 60 | 10 | 5.9 | 30.3 | 32.7 | 31.0 | 70.1 | 3.4 | 17.3 | 0.1 | ‒ | 9.1 | 38.4 | 22.8 |
| WT+Mordenite | 220 | 60 | 10 | 6.0 | 30.9 | 30.0 | 33.1 | 71.5 | 3.4 | 15.9 | 0.1 | ‒ | 9.1 | 22.8 | 27.3 |

1VM – volatile matter, 2FC – fixed carbon, 3PD – Average pore diameter measured from the desorption branch according to the BJH method.

Table S5

HHV, solid yield, carbon yield, hydrogen yield, energy yield, DC, DH, DO, EF, atomic ratios, CE and WL of the WT+Zeolite samples as compared to the WCPR.

| Samples | T, °C | t, min | H2O/WCPR ratio | HHV, MJ/kg | Solid yield, wt% | Carbon yield, wt% | Hydrogen yield, wt% | Energy yield, % | DC1, % | DH2, % | DO3, % | EF4 | Atomic ratio |  | CE5 | WL6, % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  |  | O/C | H/C |  |  |
| WCPR | ‒ | ‒ | ‒ | 20.1 | ‒ | ‒ | ‒ | ‒ | ‒ | ‒ | ‒ | 1.00 | 0.6 | 1.5 | 1.00 | – |
| WT_WCPR_220 | 220 | 60 | 10 | 22.3 | 60.0 | 68.8 | 53.2 | 66.4 | 31.2 | 41.1 | 43.2 | 1.11 | 0.5 | 1.2 | 1.15 | 40.0 |
| WT+ZSM-5 | 220 | 60 | 10 | 27.0 | 31.9 | 47.9 | 15.7 | 42.8 | 52.1 | 78.9 | 79.9 | 1.34 | 0.2 | 0.5 | 1.50 | 68.1 |
| WT+Beta | 220 | 60 | 10 | 27.0 | 30.5 | 45.4 | 15.3 | 41.0 | 54.6 | 79.5 | 82.8 | 1.34 | 0.2 | 0.5 | 1.49 | 69.5 |
| WT+Y | 220 | 60 | 10 | 25.6 | 35.0 | 47.5 | 22.8 | 44.6 | 52.5 | 71.0 | 78.7 | 1.28 | 0.2 | 0.7 | 1.36 | 65.0 |
| WT+USY | 220 | 60 | 10 | 26.7 | 32.9 | 47.7 | 18.1 | 43.7 | 52.3 | 76.0 | 81.3 | 1.33 | 0.2 | 0.6 | 1.45 | 67.1 |
| WT+Mordenite | 220 | 60 | 10 | 27.3 | 32.0 | 47.3 | 17.4 | 43.4 | 52.7 | 76.4 | 82.9 | 1.36 | 0.2 | 0.6 | 1.48 | 68.0 |

1DC – decarbonization, 2DH – dehydrogenation, 3DO – deoxygenation, 4EF – enhancement factor, 5CE – carbon enrichment, 6WL – weight loss.

Table S6

SEM-EDX analysis of the WCPR, WT_WCPR_220, and WT+Beta samples.

| WCPR |  |  |  |
| --- | --- | --- | --- |
| Element | Scan 1 (wt%) | Scan 2 (wt%) | Scan 3 (wt%) |
| C | 57.97 | 58.57 | 57.97 |
| O | 41.69 | 41.27 | 41.85 |
| Si | 0.06 | ‒ | 0.06 |
| S | 0.14 | ‒ | ‒ |
| Ca | 0.13 | ‒ | 0.13 |
| WT_WCPR_220 (220 °C after 30 min) |  |  |  |
| C | 59.42 | 59.40 | 58.75 |
| O | 40.58 | 40.60 | 41.25 |
| WT+Beta (220 °C after 30 min) |  |  |  |
| C | 45.57 | 45.15 | 46.57 |
| O | 45.45 | 44.76 | 43.72 |
| Si | 8.23 | 8.81 | 8.90 |
| Al | 0.69 | 0.71 | 0.73 |
| N | ‒ | 0.56 | ‒ |
| Ca | 0.06 |  | 0.08 |

Table S7. Comparison of higher heating value (HHV) and ultimate composition of biochar from different precursor biomass types following WT under optimal reaction conditions.

| Biomass | T, °C | Time, min | Biomass-to-liquid ratio, g:g | HHV, MJ/kg | Ultimate analysis (wt%) |  |  |  |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | C | H | O | N | S |  |
| Bamboo sawdust | ‒ | ‒ | ‒ | 17.7 | 49.2 | 6.6 | 43.1 | 0.4 |  | [1] |
|  | 230 | 30 | 1:10 | 20.8 | 53.4 | 6.2 | 40.2 | 0.1 |  |  |
| Rice husk | ‒ | ‒ | ‒ | 16.2 | 40.8 | 5.7 | 40.5 | 1.2 | ‒ | [2] |
|  | 240 | 60 | 1:20 | 18.1 | 45.8 | 5.2 | 33.1 | 0.4 | ‒ |  |
| Corn stalk | ‒ | ‒ | ‒ | 17.7 | 44.5 | 6.3 | 46.4 | 0.3 | ‒ | [3] |
|  | 220 | 30 | 1:15 | 21.2 | 53.3 | 6.0 | 40.0 | 0.4 | ‒ |  |
| Bamboo sawdust | ‒ | ‒ | ‒ | 17.7 | 49.2 | 6.6 | 43.1 | 0.4 | ‒ | [4] |
|  | 240 | 30 | 1:10 | 20.9 | 64.8 | 4.4 | 30.3 | 0.2 | ‒ |  |
| Beech | ‒ | ‒ | ‒ | 17.4 | 44.9 | 5.0 | 40.9 | 0.1 | 0.04 | [5] |
|  | 200 | 10 | 1:20 | 19.1 | 48.9 | 5.4 | 40.9 | 0.2 | 0.03 |  |
| Wheat straw | ‒ | ‒ | ‒ | 17.1 | 45.0 | 4.6 | 37.6 | 0.6 | 0.1 |  |
|  | 200 | 10 | 1:20 | 19.3 | 49.7 | 5.0 | 38.4 | 0.6 | 0.1 |  |
| Spruce | ‒ | ‒ | ‒ | 20.4 | 50.3 | 6.2 | 43.4 | 0.1 | <0.02 | [6] |
|  | 225 | 30 | 1:5 | 23.0 | 57.0 | 5.9 | 37.1 | 0.1 | <0.02 |  |
| Birch | ‒ | ‒ | ‒ | 20.0 | 48.9 | 6.4 | 44.6 | 0.1 | <0.02 |  |
|  | 225 | 30 | 1:5 | 22.9 | 56.9 | 5.9 | 42.6 | 0.1 | <0.02 |  |
| Olive trimmings | ‒ | ‒ | ‒ | 19.8 | 48.3 | 6.1 | 40.0 | 1.5 | ‒ | [7] |
|  | 250 | 30 | 1:10 | 27.2 | 60.3 | 6.3 | 28.2 | 1.8 | ‒ |  |
| Olive pulp | ‒ | ‒ | ‒ | 21.7 | 50.3 | 5.8 | 39.2 | 1.6 | ‒ |  |
|  | 250 | 30 | 1:10 | 27.6 | 62.9 | 6.3 | 24.8 | 1.7 | ‒ |  |
| Eucalyptus bark | ‒ | ‒ | ‒ | 18.1 | 45.2 | 6.4 | 48.4 | ‒ | ‒ | [8] |
|  | 300 | 120 | 1:10 | 28.9 | 72.7 | 5.1 | 22.2 | ‒ | ‒ |  |
| Palm oil empty fruit bunches | ‒ | ‒ | ‒ | 19.5 | 48.3 | 6.7 | 43.7 | 1.0 | 0.3 | [9] |
|  | 350 | 30 | 1:6.7 | 27.2 | 66.0 | 4.2 | 28.4 | 1.1 | 0.3 |  |
| Grape pomace | ‒ | ‒ | ‒ | 20.0 | 49.1 | 6.3 | 42.3 | 2.3 | ‒ | [10] |
|  | 275 | 30 | 1:4 | 28.3 | 68.3 | 5.9 | 23.5 | 2.3 | ‒ |  |
| Wheat straw | ‒ | ‒ | ‒ | 17.6 | 45.0 | 5.7 | 44.6 | 0.4 | 0.4 | [11] |
|  | 240 | 60 | 1:10 | 23.9 | 60.7 | 5.6 | 29.5 | 0.6 | 0.4 |  |
| Dried olive pomace | ‒ | ‒ | ‒ | 22.5 | 53.5 | 6.8 | 38.6 | 1.1 | ‒ | [12] |
|  | 250 | 30 | 1:6 | 27.6 | 67.8 | 6.5 | 24.3 | 1.4 | ‒ |  |
| WCPR | ‒ | ‒ | ‒ | 20.1 | 48.3 | 6.2 | 40.3 | 0.1 | 0.5 | This study |
| WT+Mordenite | 220 | 60 | 1:10 | 27.3 | 71.5 | 3.4 | 15.9 | 0.1 | ‒ |  |

References

[1]	L. Dai, C. He, Y. Wang, Y. Liu, Z. Yu, Y. Zhou, L. Fan, D. Duan, R. Ruan, Comparative study on microwave and conventional hydrothermal pretreatment of bamboo sawdust: Hydrochar properties and its pyrolysis behaviors, Energy Convers. Manag. 146 (2017) 1–7. https://doi.org/10.1016/j.enconman.2017.05.007.

[2]	S. Zhang, T. Chen, Y. Xiong, Q. Dong, Effects of wet torrefaction on the physicochemical properties and pyrolysis product properties of rice husk, Energy Convers. Manag. 141 (2017) 403–409. https://doi.org/10.1016/j.enconman.2016.10.002.

[3]	X. Wang, J. Wu, Y. Chen, A. Pattiya, H. Yang, H. Chen, Comparative study of wet and dry torrefaction of corn stalk and the effect on biomass pyrolysis polygeneration, Bioresour. Technol. 258 (2018) 88–97. https://doi.org/10.1016/j.biortech.2018.02.114.

[4]	Y. Wang, Q. Wu, L. Dai, Z. Zeng, Y. Liu, R. Ruan, G. Fu, Z. Yu, L. Jiang, Co-pyrolysis of wet torrefied bamboo sawdust and soapstock, J. Anal. Appl. Pyrolysis. 132 (2018) 211–216. https://doi.org/10.1016/j.jaap.2018.02.012.

[5]	J. Jian, Z. Lu, S. Yao, X. Li, W. Song, Comparative Study on Pyrolysis of Wet and Dry Torrefied Beech Wood and Wheat Straw, Energy and Fuels. 33 (2019) 3267–3274. https://doi.org/10.1021/acs.energyfuels.8b04501.

[6]	Q.V. Bach, K.Q. Tran, Ø. Skreiberg, T.T. Trinh, Effects of wet torrefaction on pyrolysis of woody biomass fuels, Energy. 88 (2015) 443–456. https://doi.org/10.1016/j.energy.2015.05.062.

[7]	M. Volpe, L. Fiori, From olive waste to solid biofuel through hydrothermal carbonisation: The role of temperature and solid load on secondary char formation and hydrochar energy properties, J. Anal. Appl. Pyrolysis. 124 (2017) 63–72. https://doi.org/10.1016/j.jaap.2017.02.022.

[8]	P. Gao, Y. Zhou, F. Meng, Y. Zhang, Z. Liu, W. Zhang, G. Xue, Preparation and characterization of hydrochar from waste eucalyptus bark by hydrothermal carbonization, Energy. 97 (2016) 238–245. https://doi.org/10.1016/j.energy.2015.12.123.

[9]	G.K. Parshetti, S. Kent Hoekman, R. Balasubramanian, Chemical, structural and combustion characteristics of carbonaceous products obtained by hydrothermal carbonization of palm empty fruit bunches, Bioresour. Technol. 135 (2013) 683–689. https://doi.org/10.1016/j.biortech.2012.09.042.

[10]	M. Pala, I.C. Kantarli, H.B. Buyukisik, J. Yanik, Hydrothermal carbonization and torrefaction of grape pomace: A comparative evaluation, Bioresour. Technol. 161 (2014) 255–262. https://doi.org/10.1016/j.biortech.2014.03.052.

[11]	Q. Ma, L. Han, G. Huang, Effect of water-washing of wheat straw and hydrothermal temperature on its hydrochar evolution and combustion properties, Bioresour. Technol. 269 (2018) 96–103. https://doi.org/10.1016/j.biortech.2018.08.082.

[12]	A. Missaoui, S. Bostyn, V. Belandria, B. Cagnon, B. Sarh, I. Gökalp, Hydrothermal carbonization of dried olive pomace: Energy potential and process performances, J. Anal. Appl. Pyrolysis. 128 (2017) 281–290. https://doi.org/10.1016/j.jaap.2017.09.022.

Corresponding authors:

E-mail address: andrii.kostyniuk@ki.si (Andrii Kostyniuk)